pArT I - GENERAL

- SECTION INCLUDES

  - Excavation, filling and grading.

  - Soil materials designated as topsoil

  - RELATED SECTIONS/DOCUMENTS

- Section 32 92 00 – Turf and Grasses

- Section 32 93 00 – Plants

  - REFERENCES

- Illinois Department of Transportation “Standard Specifications for Road and Bridge Construction”, latest edition, identified as IDOT.

- The USDA Ag. Handbook 60: Diagnosis and improvement of Saline and Alkali Soils.

  - QUALITY ASSURANCE

- The contractor shall engage an approved agronomic soil testing laboratory and an approved physical analysis testing laboratory to determine topsoil fertility and nutrient data, soil classifications, consistency tests of excavated materials and moisture-density.

pART 2 - PRODUCT

- SOIL MATERIALS

    - In general, soil materials shall be free of debris, roots, wood, scrap material, vegetative matter, refuse, soft unsound particles, frozen, deleterious or objectionable materials.

      - General Site Fill:  General site fill material shall be friable soil without clods of clay and shall conform to the general requirements for soil materials.

        - General site fill shall possess the characteristics required for compaction to the values of soil density herein specified for the location of intended use.  Maximum particle size shall be 3 inches.

        - General site fill shall be classified as SW, SP or SM by ASTM D2487.

        - General site fill shall have a dry maximum density of not less than 105 pounds per cubic foot per ASTM D1557.

      - Topsoil:  Topsoil which has been stripped from on-site may be utilized as topsoil on the project.  Additional topsoil required shall be furnished as specified below: